## Slide 1: Enhancing Markets for Recovered C&D Derived Products: Opportunities with C&D Fines and Wood-Derived Biochar
Timothy G. Townsend, PhD, PE Neel Kalita, Yalan Liu, Jake Thompson Department of Environmental Engineering Sciences
Engineering School for Sustainable Infrastructure and Environment University of Florida
August 26, 2020
ttown@ufl.edu
http://townsend.essie.ufl.edu

## Slide 2: Major C&D Recovered Commodities
Aggregate
Wood
Fines
Metal
Cardboard
Gypsum Drywall
Asphalt Shingles
RDF

## Slide 3: C&D Wood
Dimensional lumber
Pallets
Land clearing wood
Engineered wood
  Plywood
  MDF
  OSB
Treated wood

## Slide 5: C&D Fines
Materials screened from the mixed CDD
  Soil
  Aggregate
  Wood
  Gypsum
  Shingles
Depends on waste stream, materials removed, degree of processing
Size depends on screen size
Management options:
  Reuse as alternative daily cover at landfills
  Reuse outside of landfills
Fines
Major
Minor

## Slide 7: CDRA Fines Characterization Study
Chart: 
| Asphalt | Gypsum | Concrete | Paper | Wood | Glass | Cotton | Plastics | Steel
Asphalt Gypsum Concrete Paper Wood Glass Cotton Plastics Steel | 0.1516 | 0.050217 | 0.42898 | 0.050124 | 0.20108 | 0.11532 | 0.00034483 | 0.00099138 | 0.0013632
> 25 mm
Chart: 
| Asphalt | Gypsum | Concrete | Paper | Wood | Glass | Cotton | Plastics | Steel
 | 0.10947 | 0.10059 | 0.49577 | 0.058749 | 0.16452 | 0.036454 | 0.00021133 | 0.011095 | 0.023774
19 mm – 25 mm

## Slide 8: Potential Fines Markets and Issues
Landfill Cover
Fill material
Soil/agricultural amendment
Will it suppress fires?
Will it cause odor?
Meet fill needs?
Will it pose environmental risk?
Will it meet amendment needs?
Will it pose environmental risk?
Notes: The bunkers underneath the picking line.

## Slide 9
In some cases, beneficial use risk levels may already be provided for C&D fines

## Slide 10
Most trace components were not found to be a concern.
  Asbestos, PCBs, most metals
Four components emerge as levels of possible concern:
  Arsenic
  Lead
  Benzo-a-pyrene (BAP)
  Sulfate
CDRA Fines Characterization Results
Exposure concern
Landfill odor concern

## Slide 11: Transitioning from Managing By-Products to Developing Products
Limitations often exist to the reuse of C&D fines
Opportunities to reduce pollutant concentrations:
  Be more selective on the waste processed
  Target specific size fractions
  Washing
  Blending
What about the gypsum drywall problem when the desired market is landfill daily cover?

## Slide 12: The Challenge of Gypsum Drywall in Landfills
Issues with Hydrogen Sulfide (H2S)
  Odor
  Health and safety
Gypsum
(CaSO4●2H2O)
Water

## Slide 13: Creating a Better Landfill Cover Product

## Slide 14: Biochar
Produced by pyrolysis of biomass under oxygen-limited conditions
Fine-grained and porous substances
Activated carbon and biochar is known to absorb H2S

## Slide 15: Proof of Concept Study
Objective: Explore whether addition of biochar could attenuate H2S emissions from landfilled C&D fines
Approach: Mix biochar and C&D fines in simulated landfill reactors and measure H2S generation

## Slide 16: Materials
Two C&D fines
Two biochar samples
C&D fines 1
C&D fines 2
Biochar 1
Biochar 2

## Slide 17
100ml 25ppm H2S
30g size reduced
biochar 2
30g size reduced
biochar 2
60g size reduced
biochar 2
60g size reduced
biochar 2
90g size reduced
biochar 2
90g size reduced
biochar 2
Preliminary experiment
Measure H2S
Store in dark for 3 days
250ml bottle
250ml bottle
250ml bottle
250ml bottle
Notes: Basic mechanical processing operation

## Slide 18
Twist seal cap with two valve slots
Sampling / nitrogen flushing valves
C&D fines, biochar and water
Experimental flask

## Slide 19
H2S measurement
Use a glass syringe to take H2S out of flask
Inject the gas into a tedlar bag (dilute if necessary)
Measure the H2S in the bag using a Jerome 631-X H2S analyzer
The Jerome meter has a detection range of 0.003-50ppm
The H2S was diluted using the lab air if higher than 50ppm
The Jerome meter was checked using a 25ppm H2S standard gas before measurement

## Slide 20
Results

## Slide 21
Results

## Slide 22
Results

## Slide 23
Results

## Slide 24
Results
C&D fines 2

## Slide 25: Focused Research Effort for End Market Development
Determine the optimum approach or recipe for blending C&D fines and biochar in the laboratory
Validate with pilot and field studies

## Slide 26: Summary
CDRA research has targeted market development for C&D materials; there is a need to develop products, not just manage residuals.
Past research focused on how to produce better fines.
Current research is examining the creation of products made from C&D fines and C&D-wood derived biochar.

## Slide 27: Contact Information
Timothy G. Townsend, PhD, PE
Professor
Department of Environmental Engineering Sciences
Engineering School for Sustainable Infrastructure and Environment
University of Florida
Gainesville, Florida 32608
352-392-0846
ttown@ufl.edu
nkalita@ufl.edu
http://pages.ees.ufl.edu/townsend/